TIPA

Triisopropanolamine solution 85%

—————————————————————————————————————————-------

INTRODUCTION

Isopropanolamine is a hydramine compound with orgnic amine and hydroxyl	as wellit is a general expression of Monoisopropanolamine (MIPA) , Diisopropanolamine (DIPA) , Triisopropanolamine(TIPA).

Chemical Name: 1,1’,1”-Nitrilotri-2-propanol

## CAS No.: 122-20-3

——————————————————————————————————————————-----

### PRODUCT SPECIFICATION

TIPA Content:	85% Min.

MIPA Plus DIPA:       3% Max.

Water Content:	10% - 15%.

Appearpance:	Colourless or slight yellow

Structure Formula:	C9H21NO3

————————————————————————————————————————————

### PHYSICAL AND CHEMICAL CHARACTERISTICS

Physical Form(25℃):		Liquid

Color:					Colourless or slight yellow

Freezing Point:			3-8℃

Boiling Point:				104-107℃

Smelling:					Very light ammoniacal odour

Flash Point:				Min.160℃

Specifical Gravity(25/4℃):	1.027

Viscosity (25℃):			500-600cps

——————————————————————————————————————————-----

### APPLICATIONS

Cement & Concrete	Improves the grinding efficiency resulting in energy savings; prevents from agglomeration or clumping; as water reducing agent.

Rubber curing	Chain terminator in isoprene polymerization.

Surfactants 	emulsifying additives in textile lubricants

Metal working	To improve corrosion protection, antioxidant.

——————————————————————————————————————————-----

PACKING	Packed in iron drum, net weight 215kg. Isotank and IBC packing are also available or can be specified according to customer’s requests.

----------------------------------------------------------------------------------------

STORAGE	Shelf time of TIPA 85% is one year, and after then it could still be available once has passed a chemical test.

——————————————————————————————————————————-----

SAFETY & TOXICITY

Generally present no toxicity, alkalescence but do not irritate skin.

Higher flashing point, it should be prevented the material from spilling into the eyes while handling.